SEM images were analyzed using a Python workflow based on the scikit image package [1]. The images were lightly smoothed with a Gaussian filter to reduce high frequency graininess present in the SEM data. An initial segmentation mask was then generated using local thresholding. This approach was chosen because contrast can vary across the images, which made the adaptive local threshold more adept to capture features [2]. The resulting mask was cleaned with morphological operations to remove small thresholding artifacts and fill gaps within features [3].

The cleaned mask was then converted into a labeled segmentation using connected component analysis. Individual features were measured using region property analysis in scikit image. Additional geometric filters were applied to remove remaining segmentation artifacts [1]. The main properties of interest were the major and minor axes of the equivalent ellipse fit to each segmented feature, which were used as estimates of feature length and width. These measurements were compiled and compared with AFM data to check consistency between the two measurement techniques. Standard particle characterization definitions were used to interpret the different size metrics of the two techniques [4].

Work Cited

[1]	Stéfan van der Walt et al., “scikit-image: Image Processing in Python,” PeerJ, vol. 2, 2014, doi: 10.7717/peerj.453.

[2]	Rafael C. Gonzalez and Richard E. Woods, “Digital Image Processing,” 2nd Edition., Prentice Hall, 2002, pp. 600–612.

[3]	Jean Serra, Image Analysis and Mathematical Morphology, 1st ed. London: Academic Press, 1982.

[4]	Pabst, W. and Gregorová, E., Characterization of Particles and Particle Systems. Prague, Czech Republic: Institute of Chemical Technology Prague, 2007.